## Slide 1: Coordinated In-Situ Analysis of Meteoritic Nanodiamonds
Fischer-Tropsch Fe-Ni Catalysis
Vapor Condensation from Supernovae Ejecta Precursor Flash Heating/Collisional Shock Carbon Vapor Supersaturation
Ethanol C-C Bonds are ideal Atmospheric pressure microplasma T ≈ 100 °C Residence time ≈1 ms
Havishk Tripathi1,2 Rhonda Stroud1,2, Larry Nittler1
1School of Earth and Space Exploration, ASU, Tempe, AZ
2Buseck Center for Meteorite Studies, ASU, Tempe, AZ
Methods
  Sulfur -embed
  Matrix, Microtome
References
Introduction
Initial STEM-EDXS-EELS Results
Meteoritic nanodiamonds (NDs)
carbon nanograins (2–5 nm) trapped in carbonaceous meteorites thought to be presolar
carry stellar nucleosynthetic anomalies and encode processes predating the Solar System.
Challenge
Traditional bulk analyses mask ND subpopulation variation, preventing origin(s) identification. Objective
Differentiate presolar stardust vs. solar system ND formation in carbonaceous chondrites and returned asteroid samples
  70-100 nm
  thin section
  C,N Isotopes
  In-situ aberration
  corrected STEM/TEM
EDXS (composition)
EELS (bonding)
NanoSIMS
Figure 1 (left) STEM HAADF of microtomed Ryugu particle on lacey carbon grid.
(A) Organic matter (OM) with embedded nanodiamonds (OMEN) (magenta)
(B) Petrographic context OMEN in fine grained matrix (phyllosilicates/ sulfides/diamond-free OM). Elliptical void in OMEN suggests NDs form as an interstellar icy particle rind.
Sample Prep
Imaging
Isotopic Imaging
Potential Formation Mechanisms & Distinct Isotopic Fingerprints
Circumstellar Outflow (CTTS at 1 AU)
FUV Flux (erg cm⁻² s⁻¹) (912-1700Å) ~1.6 × 10⁴
UV Flux
Figure 2
(A) Spectrum image ROI (inset) and
Extracted EDXS spectra from Amorphous C
is N-richer than ND (blue).
Cu peak = system artifact; Si/Al/Mg/Fe/O from heteroatoms in OM; residual from acid dissolution.
(B) Extracted
EELS C K-edge
From
ND (sp³)
amor-OM (sp²)
Radical Mediated Nucleation
Technical Approach
Organic ice mantles absorb FUV photons (λ < 200 nm)
H2O-rich ice + minor CH₄, CH₃OH, CO, NH₃
(1-5%)
UV Photolysis of Organic-Rich Ices
G₀ > 30
Locate ND clusters embedded in organic matter in carbonaceous chondrites and returned asteroid samples
Measure C and N isotopes of clusters to check for multiple formation histories
Mechanism | δ¹³C (‰) | δD (‰) | Key Anomalies | Viable Environment
Microplasma | -25 to -15 | +500 to +1000 | None | Presolar cloud
UV Photolysis | -35 to -15 | +100 to +1000 | None | Circumstellar
Supernova Condensation | Neutral | Low | Pt/Xe anomalies | SN ejecta only
Isotopic Signature ⇌ Origin |  |  |  | 
δ¹³C |  | δ15N |  | Viable Environment
> Solar | ~ Solar | > Solar | ~ Solar | 
✓ |  |  | ✓ | C star outflow
 | ✓ | ✓ |  | Diffuse ISM Cold Molecular Cloud
 | ✓ | ✓ |  | Outer Nebula
 | ✓ |  | ✓ | Inner Nebula
Early Solar System
active accretion
Lyα Dominated (88%)
Cold Formation Mechanisms
Hot Formation Mechanisms
Microplasma Alcohol Vapor Dissociation
HT/HP Processes
CO adsorption and activation
H₂ activation
CH₂ initiation
Carbene insertion
Chain growth
M = Fe-Ni catalytic site (metal grain surface)
Nebular conditions (~300-700K, 10⁻⁴ atm)
S. J. Desch and N. Miret-Roig, "The Sun's birth environment: Context for meteoritics," Space Sci. Rev., vol. 220, no. 7, Art. no. 76, 2024.
G. R. Huss and R. J. Lewis, "Presolar diamond, SiC, and graphite in meteorites," Geochim. Cosmochim. Acta, vol. 60, pp. 331–346, 1996.
G. R. Huss, S. T. Husa, and S. A. Sandford, "UV processing of presolar organic ices," Astrophys. J., vol. 849, p. 75, 2017.
A. Kouchi et al., "Novel routes for diamond formation in interstellar ices and meteoritic parent bodies," Astrophys. J. Lett., vol. 626, L129, 2005.
A. Kumar et al., "Formation of nanodiamonds at near-ambient conditions via microplasma dissociation of ethanol vapour," Nat. Commun., vol. 4, Art. no. 2618, 2013.
J. Llorca and I. Casanova, "CO + H₂ reaction over Fe–Ni metal at low pressures: Implications for nebular diamond formation," Geochim. Cosmochim. Acta, vol. 64, no. 15, pp. 2673–2684, 2000.
L. R. Nittler and F. Ciesla, "Astrophysics with extraterrestrial materials," Annu. Rev. Astron. Astrophys., vol. 54, pp. 53–93, 2016.
G. Pareras et al., "Single-atom catalysis in space – II. Ketene–acetaldehyde–ethanol and methane synthesis via Fischer–Tropsch chain growth," Astron. Astrophys., vol. 687, p. A230, 2024.
R. M. Stroud et al., “Electron microscopy observations of the diversity of Ryugu organic matter and its relationship to minerals at the micro‐to nano‐scale,” Meteori. & Planeta. Sci. 59 (8), 2023-2043
Outer Nebula
Diffuse ISM & Cold Molecular Cloud
Inner Nebula
r-process enriched Carbon vapor
Extreme initial condition (IC)
(P > 10 GPa)
(T ≫ 1000 K)
Cooling ejecta under low-pressure conditions (≤ atm) forms NDs to later enter presolar cloud
~10⁷
G₀
FUV Flux (erg cm⁻² s⁻¹) (912-1700Å) 0.05-5
UV Flux
~30-3000
G₀
FUV Flux (erg cm⁻² s⁻¹) (912-1700Å) 0.05-5
UV Flux
~30-3000
G₀
FUV Flux (erg cm⁻² s⁻¹) (912-1700Å) ~1.6 × 10⁴
UV Flux
~10⁷
G₀
cluster-mediated
CO–H₂ ice reactions
Photon-processed ice grains
Hydrocarbon Catalysis
on Fe-Ni grains
under solar nebula conditions
UV/H-radical Exposure
Hydrocarbon
Feedstock
)
Alkyl radicals
(
Meteoritic Nanodiamond Formation
sp² Hybridization
Diamond Nucleation
Carbon Cluster Formation
Notes: Found as trace components of primitive carbonaceous chondrites
Presolar cloud fluxes (G₀ = 30–3000) initiated chemical precursors.
- Peak CTTS fluxes (G₀ ~10⁷) optimized diamond nucleation.
FUV Range: 912–1700 Å
(far-UV photochemical region)
moderate flux + Ambient UV from nearby massive stars.
- Flux decline post-accretion/cluster dispersal halted production

## Slide 2: v
sp² Hybridization
Diamond Nucleation
Carbon Cluster Formation
UV/H-radical Exposure
Hydrocarbon
Feedstock
)
Alkyl radicals
(
Meteoritic Nanodiamond Formation